AFM Corporation

17645 Juniper Path, Suite 260

Lakeville, MN 55044

Phone: (800) 255-3908

Phone: (952) 892-0809

Fax: (952) 232-1091

www.foam-control.com

SECTION 07 21 13.13

FOam board insulation – Termite Resistant for exterior insulation finish systems

GENERAL

SUMMARY

Section includes termite resistant rigid expanded polystyrene (EPS) insulation.

Types of rigid expanded polystyrene include:

        - Foam-Control EPS with Perform Guard

REFERENCES

ASTM C 578 - Standard Specification for Rigid, Cellular Polystyrene Thermal Insulation.

ASTM E 2430 - Standard Specification For Expanded Polystyrene (EPS) Thermal Insulation Boards For Use In Exterior Insulation and Finish Systems (EIFS)

ASTM E 84 - Standard Test Method for Surface Burning Characteristics of Building Materials

ICC ES AC12 – Acceptance Criteria for Foam Plastic Insulation.

ICC ES AC239 – Acceptance Criteria for Termite-Resistant Foam Plastics.

SUBMITTALS

Submit insulation manufacturer’s product literature and installation instructions, including:

Physical properties in compliance with ASTM C578 Type I and ASTM E2430.

EPS Code Compliance: Provide ICC ES code report for EPS foam with evidence of compliance with code. Submit current compliance report numbers from ICC ES with conformance to the International Building Code (IBC) and International Residential Code (IRC).  Code report shall include compliance with ICC ES AC12 (Foam Plastic) dated June 2006 and ICC ES AC239 (Termite-Resistance) dated June 2008.

Third Party certification of flame spread and smoke developed indexes

20-year in-service, non-prorated thermal performance warranty.

15-year in-service termite resistant performance warranty.

DELIVERY, STORAGE & HANDLING

Deliver insulation in packages labeled with material Type and R-value.

Store in original unopened packaging above ground, and protected from moisture and sunlight prior to installation.

Product should not be exposed to open flame or other ignition sources.

WARRANTY

Provide Foam-Control EPS 20-year in-service, non-prorated R-value warranty covering the long-term thermal performance of expanded polystyrene insulation.

Provide Foam-Control EPS with Perform Guard 15-year in-service warranty covering the long-term performance of expanded polystyrene insulation.

PRODUCTS

MATERIAL COMPATIBILITY

The insulation must be compatible with all components of the intended application.

MANUFACTURERS/SUPPLIERS:

***Note to Specifier*** Select the name and address of the local Licensed Foam-Control EPS with Perform Guard Manufacturers/Suppliers.

    - ACH Foam Technologies, LLC, 5250 North Sherman St., Denver, CO  80216

    - ACH Foam Technologies, LLC, 111 W. Fireclay Ave., Murray, UT  84107

    - ACH Foam Technologies, LLC, 775 Waltham Way, Suite 105, McCarran, NV  89434

    - ACH Foam Technologies, LLC, 90 Trowbridge Drive, Fond du Lac, WI  54936-0660

    - ACH Foam Technologies, LLC, 4001 Kaw Drive, Kansas City, KS  66102

    - ACH Foam Technologies, LLC, 1418 Cow Palace Road, Newton, KS  67114

    - ACH Foam Technologies, LLC, 809 East 15th Street, Washington, IA  52353

    - ACH Foam Technologies, LLC, 2731 White Sulphur Road, Gainesville, GA  30501

    - Big Sky Insulations, Inc., 15 Arden Drive, Belgrade, MT  59714

    - Branch River Plastics, Inc., 15 Thurber Boulevard, Smithfield, RI  02917

    - Henry Products, Inc., 302 S. 23rd Avenue, Phoenix, AZ 85009

    - Mid-Atlantic Foam, Inc., 57 Joseph Mills Drive,  Fredericksburg, VA  22404

    - Mid-Atlantic Foam, Inc., 326 McGhee Road, Winchester, VA  22603

    - NoArk Enterprises, Inc., 10101 Highway 70 East, North Little Rock, AR  72117

    - Pacific Allied Products, Ltd., 91-110 Kaomi Loop, Kapolei, HI  96707

    - Poliestireno Alfa-Gamma S.A. DE C.V., Maquiladoras #331 Interior A y B, Tijuana, BC, Mexico, 22500

    - Poly-Foam Inc., 116 Pine Street South, Lester Prairie, MN 55354

    - Therma Foam, LLC, 1240 Hwy 77 North, Hillsboro, TX 76645

    - Thermal Foams, Inc., 2101 Kenmore Avenue, Buffalo, NY 14207

    - Thermal Foams/Syracuse, Inc., 6173 South Bay Road, Cicero, NY 13039

AFM Corporation, 17645 Juniper Path, Suite 260, Lakeville, MN 55044

INSULATION

Foam-Control EPS with Perform Guard in compliance with ASTM C578 Type I and ASTM E2430.

Foam-Control EPS with Perform Guard  with flame spread of less than 25 and a smoke developed index of less than 450

Foam-Control EPS with Perform Guard  Insulation:

        - Thickness _____.

        - R-value _____.

All Foam-Control EPS with Perform Guard shall be treated by the manufacturer with a tested and proven termite treatment for below grade applications, 3 year minimum field exposure.  The treatment shall be EPA registered, meet requirements of ICC ES AC239, and be recognized in an ICC ES report.

EXECUTION

INSTALLATION

Installation: [ Specify instructions to suit project requirements. ].

END OF SECTION