AFM Corporation

17645 Juniper Path, Suite 260

Lakeville, MN 55044

Phone: (800) 255-3908

Phone: (952) 892-0809

Fax: (952) 232-1091

www.foam-control.com

SECTION 07 21 13.13

FOam board insulation

GENERAL

SUMMARY

Section includes rigid expanded polystyrene (EPS) insulation.

Types of rigid expanded polystyrene include:

        - Foam-Control EPS

REFERENCES

ASTM C 578 - Standard Specification for Rigid, Cellular Polystyrene Thermal Insulation.

ASTM E 84 - Standard Test Method for Surface Burning Characteristics of Building Materials

ICC ES AC12 – Acceptance Criteria for Foam Plastic Insulation.

SUBMITTALS

Submit insulation manufacturer’s product literature and installation instructions, including:

Physical properties in compliance with ASTM C578 Type specified.

EPS Code Compliance: Provide ICC ES code report for EPS foam with evidence of compliance with code. Submit current compliance report numbers from ICC ES with conformance to the International Building Code (IBC) and International Residential Code (IRC).  Code report shall include compliance with ICC ES AC12 (Foam Plastic) dated June 2006.

Third Party certification of flame spread and smoke developed indexes

20-year in-service, non-prorated thermal performance warranty.

DELIVERY, STORAGE & HANDLING

Deliver insulation in packages labeled with material Type and R-value.

Store in original unopened packaging above ground, and protected from moisture and sunlight prior to installation.

Product should not be exposed to open flame or other ignition sources.

WARRANTY

Provide Foam-Control EPS 20-year in-service, non-prorated R-value warranty covering the long-term thermal performance of expanded polystyrene insulation.

PRODUCTS

MATERIAL COMPATIBILITY

The insulation must be compatible with all components of the intended application.

MANUFACTURERS/SUPPLIERS:

***Note to Specifier*** Select the name and address of the local Licensed Foam-Control EPS Manufacturers/Suppliers.

ACH Foam Technologies, LLC, 5250 North Sherman St., Denver, CO  80216

ACH Foam Technologies, LLC, 111 W. Fireclay Ave., Murray, UT  84107

ACH Foam Technologies, LLC, 775 Waltham Way, Suite 105, McCarran, NV  89434

ACH Foam Technologies, LLC, 90 Trowbridge Drive, Fond du Lac, WI  54936-0660

ACH Foam Technologies, LLC, 4001 Kaw Drive, Kansas City, KS  66102

ACH Foam Technologies, LLC, 1418 Cow Palace Road, Newton, KS  67114

ACH Foam Technologies, LLC, 809 East 15th Street, Washington, IA  52353

ACH Foam Technologies, LLC, 2731 White Sulphur Road, Gainesville, GA  30501

Big Sky Insulations, Inc., 15 Arden Drive, Belgrade, MT  59714

Branch River Plastics, Inc., 15 Thurber Boulevard, Smithfield, RI  02917

Henry Products, Inc., 302 S. 23rd Avenue, Phoenix, AZ 85009

Mid-Atlantic Foam, Inc., 57 Joseph Mills Drive,  Fredericksburg, VA  22404

Mid-Atlantic Foam, Inc., 326 McGhee Road, Winchester, VA  22603

NoArk Enterprises, Inc., 10101 Highway 70 East, North Little Rock, AR  72117

Pacific Allied Products, Ltd., 91-110 Kaomi Loop, Kapolei, HI  96707

Poliestireno Alfa-Gamma S.A. DE C.V., Maquiladoras #331 Interior A y B, Tijuana, BC, Mexico, 22500

Poly-Foam Inc., 116 Pine Street South, Lester Prairie, MN 55354

Therma Foam, LLC, 1240 Hwy 77 North, Hillsboro, TX 76645

Thermal Foams, Inc., 2101 Kenmore Avenue, Buffalo, NY 14207

Thermal Foams/Syracuse, Inc., 6173 South Bay Road, Cicero, NY 13039

AFM Corporation, 17645 Juniper Path, Suite 260, Lakeville, MN 55044

INSULATION

Foam-Control EPS in compliance with ASTM C578.

Foam-Control EPS with flame spread of less than 25 and a smoke developed index of less than 450

Select one or more of the Insulation Types from the listings as follows, as required by the project:

Foam-Control EPS Insulation: ASTM C578 [Type I, 0.90 pcf min.], [Type VIII, 1.15 pcf min.], [Type II, 1.35 pcf min.], [Type IX, 1.80 pcf min.].

        - Thickness _____.

        - R-value _____.

THERMAL BARRIER

A thermal barrier must be installed as required by code.

***Note to Specifier***  Some applications may not require a thermal barrier.  For these applications, please refer to ICC ES report.

EXECUTION

INSTALLATION

    - Installation: [ Specify instructions to suit project requirements. ].

END OF SECTION