AFM Corporation

17645 Juniper Path, Suite 260

Lakeville, MN 55044

Phone: (800) 255-3908

Phone: (952) 892-0809

Fax: (952) 232-1091

www.geofoam.com

SECTION 31 23 23.43

EPS GEOFOAM

GENERAL

  - SUMMARY

    - Section includes expanded polystyrene (EPS) Geofoam.

    - Related Sections: Section(s) related to this section include:

      - Earthworks:  Division 31 Earthworks sections.

  - REFERENCES

    - ASTM D6817 - Standard Specification for Rigid, Cellular Polystyrene Geofoam.

  - SUBMITTALS

    - Submit EPS Geofoam manufacturer’s product literature and TechData, including:

      - Physical properties in compliance with ASTM D6817 Type specified.

      - 10-year physical property warranty.

    - Shop drawings showing EPS Geofoam block layout.

    - Quality Assurance: Submit the following:

      - Test Compliance: Summary of test compliance with specified performance characteristics and physical properties.

      - Certificates: Manufacturer shall supply a product certificate showing evidence of Third Party Quality Control.

  - DELIVERY, STORAGE & HANDLING

    - Deliver EPS Geofoam labeled with material Type.

    - Store above ground, and protected from moisture and sunlight prior to installation.

    - Product should not be exposed to open flame or other ignition sources.

  - WARRANTY

    - Provide EPS Geofoam 10-year warranty covering the long-term physical property of expanded polystyrene Geofoam.

PRODUCTS

***Note to Specifier*** Select the name and address of the local Licensed Foam-Control EPS Geofoam Manufacturers/Suppliers.

  - Manufacturers/Suppliers:

    - ACH Foam Technologies, LLC, 5250 North Sherman St., Denver, CO  80216

    - ACH Foam Technologies, LLC, 111 W. Fireclay Ave., Murray, UT  84107

    - ACH Foam Technologies, LLC, 775 Waltham Way, Suite 105, McCarran, NV  89434

    - ACH Foam Technologies, LLC, 90 Trowbridge Drive, Fond du Lac, WI  54936-0660

    - ACH Foam Technologies, LLC, 4001 Kaw Drive, Kansas City, KS  66102

    - ACH Foam Technologies, LLC, 1418 Cow Palace Road, Newton, KS  67114

    - ACH Foam Technologies, LLC, 809 East 15th Street, Washington, IA  52353

    - ACH Foam Technologies, LLC, 2731 White Sulphur Road, Gainesville, GA  30501

    - Big Sky Insulations, Inc., 15 Arden Drive, Belgrade, MT  59714

    - Branch River Plastics, Inc., 15 Thurber Boulevard, Smithfield, RI  02917

    - Henry Products, Inc., 302 S. 23rd Avenue, Phoenix, AZ 85009

    - Mid-Atlantic Foam, Inc., 57 Joseph Mills Drive,  Fredericksburg, VA  22404

    - Mid-Atlantic Foam, Inc., 326 McGhee Road, Winchester, VA  22603

    - NoArk Enterprises, Inc., 10101 Highway 70 East, North Little Rock, AR  72117

    - Pacific Allied Products, Ltd., 91-110 Kaomi Loop, Kapolei, HI  96707

    - Poliestireno Alfa-Gamma S.A. DE C.V., Maquiladoras #331 Interior A y B, Tijuana, BC, Mexico, 22500

    - Poly-Foam Inc., 116 Pine Street South, Lester Prairie, MN 55354

    - Therma Foam, LLC, 1240 Hwy 77 North, Hillsboro, TX 76645

    - Thermal Foams, Inc., 2101 Kenmore Avenue, Buffalo, NY 14207

    - Thermal Foams/Syracuse, Inc., 6173 South Bay Road, Cicero, NY 13039

    - AFM Corporation, 17645 Juniper Path, Suite 260, Lakeville, MN 55044

  - EPS GEOFOAM

    - Foam-Control EPS Geofoam in compliance with ASTM D6817.

    - Select one or more of the Foam-Control EPS Geofoam Types from the listings as follows, as required by the project:

      - Foam-Control EPS Geofoam: ASTM D6817 [Type EPS12], [Type EPS15], [Type EPS22], [Type EPS29], [Type EPS39], [Type EPS46].

    - All Foam-Control EPS Geofoam blocks shall be treated by the manufacturer with a tested and proven termite treatment for below grade applications, 3 year minimum field exposure.  The treatment shall be EPA registered, meet requirements of ICC ES AC239, and be recognized in an ICC ES report.

  - GEOGRIPPER PLATES

    - GeoGripper® plates shall be used to restrain EPS Geofoam from moving laterally in layer over layer applications.  The  GeoGripper plate shall be manufactured by AFM Corporation.  The plate shall be made of galvanized or stainless steel with two-sided multi-barbed design capable of piercing geofoam.  Each plate shall be capable of a lateral holding strength of 60 lbs.

***Note to Specifier*** It is the responsibility of the designer/engineer to determining the suitability and number of GeoGripper Plates.  Two plates for each 4’ x 8’ section of EPS block is a minimum recommendation to minimize block to block movement during installation.

EXECUTION

  - MANUFACTURER’S INSTRUCTIONS

    - Compliance: Comply with manufacturer’s EPS Geofoam product data; including technical bulletins.

  - PREPARATION AND INSTALLATION

    - Site Verification of Conditions: Verify conditions of substrate, grade and other conditions which affect installation of geofoam.

    - Installation: [ Specify instructions to suit project requirements. ].

  - PROTECTION

    - Protection: Protect installed product and finish surfaces from damage during construction as required.

END OF SECTION