AFM Corporation

17645 Juniper Path, Suite 260

Lakeville, MN 55044

Phone: (952) 892-0809

Fax: (952) 232-1091

www.r-control.com

SECTION 06 12 00

Structural Insulated Panels

GENERAL

SUMMARY

Section Includes: Structural Insulated Panels (SIPs).

Related Sections: Section(s) related to this section include:

Section 06 10 00 Rough Carpentry

Section 06 09 00 Wood and Plastics Fastenings

SYSTEM DESCRIPTION

Structural Insulated Panels (SIPs) consist of oriented strand board (OSB) laminated with structural adhesives to a termite resistant EPS insulation core, a EPA registered treatment for mold, mildew, and termites, and SIP Manufacturer supplied connecting splines, sealants, and SIP screws.

REFERENCES

ACSE 7 - Minimum Loads for Buildings and other Structures.

ASTM C578 – Standard Specification for Rigid, Cellular Polystyrene Thermal Insulation.

DOC PS2 – Performance Standard for Wood-based Structural-Use Panels.

ICC ES AC04 – Acceptance Criteria for Sandwich Panels.

ICC ES AC05 – Acceptance Criteria for Sandwich Panel Adhesives.

ICC ES AC12 – Acceptance Criteria for Foam Plastic Insulation.

ICC ES AC239 – Acceptance Criteria for Termite-Resistant Foam Plastics.

AWPA E1 - Standard Method for Laboratory Evaluation to Determine Resistance to Subterranean Termites.

AWPA E12- Standard Method of Determining Corrosion of Metal in Contact with Treated Wood.

ASTM D3273 - Standard Test Method for Resistance to Growth of Mold on the Surface of Interior Coatings in an Environmental Chamber.

EPA - Registered products listing.

DESIGN REQUIREMENTS

Provide SIPs which have been manufactured, fabricated and installed to withstand loads [Specify code/standard reference.] and to maintain [Specify performance criteria.] performance criteria stated by SIP manufacturer without defects, damage or failure.

SUBMITTALS

Product Data: Submit product data for specified products.

SIP Code Compliance: Provide ICC ES code report for SIP with evidence of compliance with code requirements as an alternate method of construction. Submit current compliance report number from ICC ES showing conformance to the 2012 International Building Code (IBC) and International Residential Code (IRC).  Code report shall include compliance with ICC ES AC04 (Sandwich Panels) dated February 2012.

EPS Code Compliance: Provide ICC ES code report for EPS foam with evidence of compliance with code. Submit current compliance report numbers from ICC ES with conformance to the 2012 International Building Code (IBC) and International Residential Code (IRC).  Code report shall include compliance with ICC ES AC12 (Foam Plastic) dated February 2011 and ICC ES AC239 (Termite-Resistance) dated October 2008.

Manufacturer’s Instructions:  SIP Manufacturer’s Construction Manual and load design charts.

Calculations: Provide structural calculations by a registered architect or professional engineer [in the state of] qualified to perform such work.

Shop Drawings: Submit shop drawings for SIPs showing layout, elevations, product components and accessories.

Quality Assurance Submittals: Submit the following:

Certificate: Product certificate showing compliance to Third Party Quality Control program of PFS Corp.

Fire Resistant Assemblies:  PFS construction number for each fire-rated assembly

Warranty:  Warranty documents specified herein.

QUALITY ASSURANCE

Installer Qualifications: Installer should be experienced in performing work of this section and should have specialized in installation of work similar to that required for this project.

Source Limitations:  Obtain all SIPs through one source.  All accessories to be as furnished or recommended by the SIP manufacturer.

Regulatory Requirements:

SIPs shall be recognized for compliance with [International Building Code, International Residential Code, or specify] in a current ICC ES evaluation report

Pre-installation Meeting: Conduct pre-installation meeting to verify project requirements, foundation/structural system/substrate conditions, SIP manufacturer installation instructions and SIP manufacturer warranty requirements. Comply with Division 1 Project Management and Coordination (Project Meetings) Section.

DELIVERY, STORAGE & HANDLING

Ordering: Comply with SIP manufacturer ordering instructions and lead time requirements to avoid construction delays.

Delivery: Deliver materials from SIP manufacturer with identification labels or markings intact.

Off-load SIPs from truck and handle using fork lift or other means to prevent damage to SIPs.

SIPs shall be fully supported in storage and prevented from contact with the ground.  Stack SIPs on pallets or a minimum of three stickers for every 8 feet of SIP length.

SIPs shall be fully protected from weather.  Protect against exposure to rain, water, dirt, mud, and other residue that may affect SIP performance.  Cover stored SIPs with breathable protective wraps. SIPs shall be stored in a protected area.

WARRANTY

Project Warranty: Refer to Conditions of the Contract for project warranty provisions.

Manufacturer’s Warranty: Submit SIP manufacturer’s standard warranty document. SIP Manufacturer warranty is in addition to, and not a limitation of, other rights Owner may have under Contract Documents.

Warranty Period: [Specify term.] years commencing on Date of Substantial Completion.

PRODUCTS

***Note to Specifier*** Select the name and address of the local Licensed R-Control SIP Manufacturers/Suppliers.

Manufacturers/Suppliers:

ACH Foam Technologies, LLC, 5250 North Sherman St., Denver, CO  80216

ACH Foam Technologies, LLC, 111 W. Fireclay Ave., Murray, UT  84107

ACH Foam Technologies, LLC, 775 Waltham Way, Suite 105, McCarran, NV  89434

ACH Foam Technologies, LLC, 90 Trowbridge Drive, Fond du Lac, WI  54936-0660

ACH Foam Technologies, LLC, 4001 Kaw Drive, Kansas City, KS  66102

ACH Foam Technologies, LLC, 1418 Cow Palace Road, Newton, KS  67114

ACH Foam Technologies, LLC, 809 East 15th Street, Washington, IA  52353

ACH Foam Technologies, LLC, 2731 White Sulphur Road, Gainesville, GA  30501

Big Sky Insulations, Inc., 15 Arden Drive, Belgrade, MT  59714

Branch River Plastics, Inc., 15 Thurber Boulevard, Smithfield, RI  02917

Energy Systems, Inc. 990 Epco Dr., Dandridge, TN 37725

Mid-Atlantic Foam, 326 McGhee Road, Winchester, VA 22603

NoArk Enterprises, Inc., 10101 Highway 70 East, North Little Rock, AR  72117

Thermal Foams, Inc., 2101 Kenmore Avenue, Buffalo, NY 14207

AFM Corporation, 17645 Juniper Path, Suite 260, Lakeville, MN 55044

Materials

SIPs consisting of the following:

UL certified EPS core with Perform Guard treatment, minimum of 0.95 pcf (15.2 kg/m3) complying with ASTM C578 Type I and having ICC ES recognition of termite resistance.  Insulation manufacturer shall provide Third Party UL certificate.  ICC ES report shall be provided for recognition of termite resistance in compliance with ICC AC239.

OSB identified with APA or TECO performance mark with Exposure I durability rating and performance in accordance with DOC PS-2 span rating 24/16 or greater.

Adhesives shall be in conformance with ICC ES AC05 – Acceptance Criteria for Sandwich Panel Adhesives

FrameGuard treatment for mold, mildew, and termite resistance meeting the following requirements:

        - Registered with EPA.

        - Mold growth: 0 rating, tested to ASTM D3273 for 8 weeks at 77 degrees F and 100 percent relative humidity.

        - Termite resistance: Minimum rating of 7.0, tested to AWPA E-1.

        - Corrosion potential for metals in contact with treated wood: Maximum 2 mils per year, tested to AWPA E12 for minimum of 60 days on aluminum 2024, carbon steel, hot-dip galvanized steel, and G90 galvanized steel.

        - Equivalent lateral resistance and tooth holding capacity as untreated wood.

Accessories

Splines: OSB, block splines, or I-beam for use in joining SIPs shall be supplied by SIPs manufacturer.

Fasteners:  corrosion resistant SIP screws compatible with SIP system shall be provided by the SIPs manufacturer.

      - Wood Screws for attachment to wood members

      - Heavy Duty Metal Screws for attachment to metal members (16 gauge to 3/16”)

      - Light Duty Metal Screws for attachment to metal decks (18 gauge or thinner)

SIP Sealant:  Shall be specifically designed for use with SIPs.  Sealant must be compatible with all components of the SIP.  Sealant shall be provided by the SIP manufacturer.  VOC content of SIP sealant shall be less than 10 g/L.

Dimensional Lumber:  SPF, #2 or better, or engineered equivalent unless otherwise required by structural drawings.

Vapor Barrier SIP Tape:  woven and coated polyolefin membrane with synthetic adhesive suitable for indoor use, min. 4 inch wide for use on SIP joints as specified by designer.  SIP Tape shall be supplied by the SIP manufacturer.

Fabrication

Sizes:  SIPs shall be fabricated in accordance with approved Shop Drawings

Thermal Resistance, R-value

***Note to Specifier*** Select the R-value as required for each area of construction.

      - 4 1/2” (114 mm) thick SIP with R-value of 15 at 75oF (16 at 40oF)

      - 6 1/2” (165 mm) thick SIP with R-value of 23 at 75oF (24 at 40oF)

      - 8 1/4” (210 mm) thick SIP with R-value of 29 at 75oF (32 at 40oF)

      - 10 1/4“  (260 mm) thick SIP with R-value of 37 at 75oF (40 at 40oF)

      - 12 1/4” (311 mm) thick SIP with R-value of 45 at 75oF (48 at 40oF)

***Note to Specifier*** SIPs can be designed for use as 1 hour fire resistant assemblies. See technical information publications from SIP manufacturer.

Fire Performance Rating: [Specify fire performance rating.].

***Note to Specifier*** Edit article below to suit project requirements. If substitutions are permitted, edit text below. Add text to refer to Division 1 Project Requirements (Product Substitutions Procedures) Section.

PRODUCT SUBSTITUTIONS

Substitutions: No substitutions permitted without fourteen day (14) prior approval.

RELATED MATERIALS

Related Materials: Refer to other sections for related materials as follows:

Dimensional Lumber: SPF #2 or better or pre-engineered equivalent: Refer to Division 6 Carpentry Sections.

SOURCE QUALITY

Source Quality Assurance: Each SIP component required shall be supplied by SIP manufacturer and shall be obtained from selected SIP manufacturer or its approved supplier.

Each SIP shall be labeled indicating PFS Third Party certification.

Provide evidence of UL Third Party inspection and labeling of all insulation used in manufacture of SIPs.

SIP manufacturer shall provide Lamination, R-Value and mold/mildew/termite resistance warranty documents for building owner acceptance. Manufacturer standard forms will be submitted.

Provide SIPs with Foam-Control EPS with Perform Guard for termite resistance. Treatment shall be EPA registered with treatment efficacy substantiated by ICC ES report.

Provide SIPs with FrameGuard treatment for mold, mildew, and termite resistance. Treatment shall be EPA registered with treatment efficacy substantiated by independent research.

Dimensional Tolerance - shall comply with values listed in the manufacturer’s Quality Control Manual.

Source Quality: Obtain SIPs from a single manufacturer.

EXECUTION

MANUFACTURER’S INSTRUCTIONS

Compliance: Comply with manufacturer’s ICC ES report, Load Design Charts, Construction Manual, Shop Drawings, and product data, including product technical bulletins, for installation.

Plans shall be reviewed by a qualified architect/engineer and shall be signed and/or sealed. Deviations from standard detail and load design values shall be calculated and signed and/or sealed by a qualified architect/engineer.

EXAMINATION

Site Verification of Conditions: Verify substrate conditions (which have been previously installed under other sections) are acceptable for product installation in accordance with manufacturer’s instructions.

Verify conditions of foundation/structural system/substrate and other conditions which affect installation of SIPs. Any adverse conditions shall be reported in writing. Do not proceed with installation until adverse conditions are corrected.

INSTALLATION

SIP Installation:

***Note to Specifier*** Complete installation recommendations are available from the manufacturer. SIP weight and contractor preference will dictate the erection method used. The use of a crane or lift truck may be required for SIP placement. Consult with SIP manufacturer for recommended handling methods. Supplementary lifting clamps and attachments to be provided by the contractor.

SIP Supports: Provide level and square foundation/structural system/substrate that support wall and/or roof SIPs. For wall SIPs, hold sill plate back from edge of rim board 7/16" (11 mm) to allow full bearing of OSB skins. Provide 1 1/2" (38 mm) diameter access holes in plating to align with electrical wire chases in SIPs. Provide adequate bracing of SIPs during erection. Remove debris from plate area prior to SIP placement.

SIP Fastening: Connect SIPs by nails as shown on drawings.  SIP sealant must be used together with each fastening techniques. Where SIP Screw Fasteners are used, provide a minimum of 1" (25.4 mm) penetration into support. Join SIPs using plates and splines. Secure attachment with nails, staples, or screws, and SIP sealant.  Apply SIP sealant following SIP manufacturer recommendations.

SIP Tape: Provide SIP Tape at joints between SIP panels and at intersection of SIP roof and wall.

Vapor Retarders: Provide vapor retarders mandated by building code or climate conditions.

Thermal Barriers: Interior surfaces of SIPs shall be finished with a minimum 15-minute thermal barrier, such as 1/2" (13 mm) gypsum wallboard, nominal 1" (25 mm) wood paneling, or other approved materials. Apply code approved thermal barriers according to SIP manufacturer’s recommendations.

Restrictions: Do not install SIPs directly on concrete. Do not put plumbing in SIPs without consulting SIP manufacturer. Do not overcut skins for field-cut openings and do not cut skins for electrical chases.  SIPs shall be protected from exposure to solvents and their vapors that damage the EPS foam core.

Remove and replace insulated wall or roof SIPs which have become excessively wet or damaged before proceeding with installation of additional SIPs or other work.

FIELD QUALITY REQUIREMENTS

Manufacturer’s Field Services: Upon Owner’s request, provide manufacturer’s field service consisting of product use recommendations and periodic site visits for inspection of product installation in accordance with manufacturer’s instructions.

Site Visits: [Specify number and duration of periodic site visits.].

PROTECTION

Protection: Protect installed product and finish surfaces from damage during construction.

Roof SIPs: Protect roof SIPs from weather.  Provide temporary protection at the end of the day or when rain or snow is imminent.

After installation, cover SIPs to prevent contact with water on each exposed SIP edges and faces.

END OF SECTION